## Slide 1
Analysis of GNDs beneath indents of different depth using EBSD tomography
E. Demir, S. Zaefferer, F. Roters, D. Raabe
Department of Microstructure Physics and Metal Forming
Düsseldorf, Germany
d.raabe@mpie.de
27. October 2009, MS&T, Pittsburgh

## Slide 2
Overview
Methods (3D EBSD, CP-FEM)
Characterization
Orientation gradients and dislocation analysis
Discussion
Dierk Raabe, MS&T, Pittsburgh, 27. Oct. 2009, MPIE

## Slide 3
Relationship between ISE and GND: hardness and GND in the same experiment
Indents of different depths, Cu single crystal
3D EBSD: plastic volume, orientation gradients, GNDs
Motivation and approach: specific

## Slide 4
Raabe, Zhao, Park, Roters: Acta Mater. 50 (2002) 421
Multiscale crystal plasticity FEM

## Slide 5
Nanoindentation
[-110]
[11-2]
[111]
Wang, Raabe, Klüber, Roters: Acta Mater. 52 (2004) 2229
60° conical, tip radius 1μm, loading rate 1.82mN/s, loads of 4000μN, 6000μN, 8000μN and 10000μN

## Slide 6: 3D electron microscopy, 3D EBSD, tomography
J. Konrad, S. Zaefferer, D. Raabe, Acta Mater. 54 (2006) 1369
Zaefferer,. Wright, Raabe, Metall. Mater. Trans. A 39A (2008) 374

## Slide 7
[-110]
[111]
[11-2]
Misorientation angle
0°
20°
Crystal orientation distribution around nanoindents
Zaafarani, Raabe, Roters, Zaefferer: Acta Mater. 56 (2008) 31
Cu, 60° conical, tip radius 1μm, loading rate 1.82mN/s, loads: 4000μN, 6000μN, 8000μN, 10000μN

## Slide 8
scan 7
scan 8
scan 9
Comparison, crystal rotations about [11-2] axis
viscoplastic
CPFEM
experiment
3D EBSD
dislocation-based
CPFEM
experiment
simulation
[-110]
[111]
[11-2]
Zaafarani, Raabe, Singh, Roters, Zaefferer: Acta Mater. 54 (2006) 1707
Zaafarani, Raabe, Roters, Zaefferer: Acta Mater. 56 (2008) 31

## Slide 9
Simplify
Zaafarani, Raabe, Roters, Zaefferer: Acta Mater. 56 (2008) 31

## Slide 10
From local misorientations to GNDs
misorientation
orientation gradient
(spacing d from EBSD scan)
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559
orientation difference
misorientation angle
0°
20°

## Slide 11
From local misorientations to GNDs
distortion
(sym, a-sym)
dislocation tensor (GND)
J. F. Nye. Some geometrical relations in dislocated crystals. Acta Metall. 1:153, 1953.
E. Demir, D. Raabe, N. Zaafarani, S. Zaefferer: Acta Mater. 57 (2009) 559–569
E. Kröner. Kontinuumstheorie der Versetzungen und Eigenspannungen (in German). Springer, Berlin, 1958.
E. Kröner. Physics of defects, chapter Continuum theory of defects, p.217. North-Holland Publishing, Amsterdam, Netherlands, 1981.
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559

## Slide 12
From local misorientations to GNDs
Frank loop through area r
DDT in terms of 18 b,t combinations
DDT in terms of 9 b,t combinations
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559

## Slide 13
Distribution of GNDs for different gradient resolutions
center section, 2D analysis, color code: GND density (decadic log. (1/m2) )
50 nm
100 nm
200 nm
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559

## Slide 14
Reference volumes (red color) indicates the plastic volume using lower threshold of GNDs of 1014/m2
Identification of the plastic volume
depth [mm]
center section, 2D analysis, color code: GND density (decadic log. (1/m2) )
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559

## Slide 15
Extract geometrically necessary dislocations
Demir, Raabe, Zaafarani, Zaefferer: Acta Mater. 57 (2009) 559

## Slide 16
GNDs have inhomogeneous distribution below indents with very high local density values.
Total GND density below indents drops with decreasing indentation depths. Observation contradicts strain gradient theory.
Conclusions