## Slide 1
Düsseldorf, Germany
WWW.MPIE.DE
d.raabe@mpie.de
Dierk Raabe
D. Raabe, I. Gutierrez-Urrutia
Effect of strain path and texture on microstructure in
Fe–22 wt.% Mn–0.6 wt.% C TWIP steel

## Slide 2
Electron channeling contrast imaging
Twinning and texture
Strain path effects
Bauschinger effects
Conclusions
Overview
www.mpie.de

## Slide 3
Kippwinkel
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Scripta Materialia 61 (2009), 737
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Materials Science and Engineering A 527 (2010), 3552
C. Herrera et al. Acta Materialia 59 (2011) 4653
EBSD: Work hardening of TWIP steels, Fe-22Mn-0.6C (wt%)
Dislocations in SEM

## Slide 4
Overview
www.mpie.de
Electron channeling contrast imaging
Twinning and texture
Strain path effects
Bauschinger effects
Conclusions

## Slide 5
Influence of grain orientation on deformation twinning
Tensile test
s: 380 MPa
e: 0.1
TA
IPF
Grain orientations
twins
no twins
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Scripta Materialia 61 (2009), 737
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Materials Science and Engineering A 527 (2010), 3552

## Slide 6
Tensile test
s: 950 MPa
e: 0.4
twins
no twins
TA
IPF
Grain orientations
Influence of grain orientation on deformation twinning

## Slide 7
Tensile test
s: 950 MPa
e: 0.4
twins
no twins
TA
Local stress concentrations at GB
Micromechanical B.C.
matter
twin transfer
Why twinning in these orientations?
Influence of grain orientation on deformation twinning

## Slide 8
Tensile test
s: 950 MPa
e: 0.4
twins
no twins
TA
no twin transfer
Influence of grain orientation on deformation twinning

## Slide 9
Overview
www.mpie.de
Electron channeling contrast imaging
Twinning and texture
Strain path effects
Bauschinger effects
Conclusions

## Slide 10
SD
ND
Cell Block formation
e: 0.1
<001>//shear direction
Influence of strain path: tensile vs shear on disloc. substructure

## Slide 11
e: 0.1
SD
ND
1.2
2.8
1.2
2.3
2.4
1.8
1.7
3.6
1.2
B
B
B
B
B
B
B
B
B
Misorientation profile
Influence of strain path: tensile vs shear on disloc. substructure

## Slide 12
EBSD does not detect dislocation cells
Shear : e:0.3
SD
ND

## Slide 13
Shear : e:0.3
{111} traces of shear
Substructures with misorientation up to 2deg, hence, visible via EBSD
Misorientation profile
<111>//Shear direction
Influence of strain path: tensile vs shear on disloc. substructure
ECCI
I. Gutierrez-Urrutia et al. Scripta Materialia 61 (2009), 737

## Slide 14: Influence of strain path: tensile vs shear on dislocation substructure
Tensile: dislocation cells
Shear: symmetric patterning, cell blocks, shear bands
Tensile axis
Shear direction
112
e:0.3
SD
ND
I. Gutierrez-Urrutia et al. Scripta Materialia 61 (2009), 737

## Slide 15: Influence of strain path: tensile vs shear on disloc. substructure
Tensile axis
Shear
bands
Tensile: dislocation cells
Shear: symmetric patterning, cell blocks, shear bands
e:0.3
SD
ND
I. Gutierrez-Urrutia et al. Mater.Sc Eng. A 527 (2010) 3552
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Scripta Materialia 61 (2009), 737
I. Gutierrez-Urrutia, S. Zaefferer, D. Raabe; Materials Science and Engineering A 527 (2010), 3552

## Slide 16
Overview
www.mpie.de
Electron channeling contrast imaging
Twinning and texture
Strain path effects
Bauschinger effects
Conclusions

## Slide 17: Strain reversion: Bauschinger test
e: 0.1 + (-0.03)
Cell block formation is enhanced
112
I. Gutierrez-Urrutia et al. Mater.Sc Eng. A 527 (2010) 3552

## Slide 18
e: 0.1 + (-0.03)
Cell block formation is enhanced (leading to pronounced subgrain structure)
Strain reversal leads to higher misoriented dislocation substructures
Strain reversion: Bauschinger test
I. Gutierrez-Urrutia et al. Mater.Sc Eng. A 527 (2010) 3552

## Slide 19: Strain reversion: Bauschinger test
e: 0.1 + (-0.03)
(not TEM)
ECCI image
{111} trace
GN boundaries
stat. boundaries
We identify both GN and incidental boundaries!
I. Gutierrez-Urrutia et al. Mater.Sc Eng. A 527 (2010) 3552

## Slide 20
Overview
www.mpie.de
Electron channeling contrast imaging
Twinning and texture
Strain path effects
Bauschinger effects
Conclusions

## Slide 21: Conclusions
Joint use of ECCI & EBSD
Unexpected deformation twinning
Dependence of dislocation substructure on strain path and orientation
<111>//deformation axis leads to planar dislocation substructures: DDWs structures in tension and Taylor lattice in shear
<001>//deformation axis leads to wavy dislocation substructures: cells in tension and cell block in shear
Strain reversal promotes cell block/subgrain formation with increased misorientation
Cell blocks formed by geometrically necessary boundaries along {111} planes and incidental boundaries created by statistically stored dislocations are visible via ECCI. We can estimate boundary spacings and therefore, its contribution to work-hardening.
I. Gutierrez-Urrutia et al. Mater.Sc Eng. A 527 (2010) 3552