## Slide 1
O. Dmitrieva, D. Ponge, G. Inden, J. Millán, P. Choi, D. Raabe
Düsseldorf, Germany
WWW.MPIE.DE
d.raabe@mpie.de
Dierk Raabe
Chemical gradients across martensite/austenite phase boundaries in precipitation hardened TRIP steel studied by atom probe tomography

## Slide 2
Motivation and alloy design
Atom probe tomography
Mechanical properties and microstructure
Mn partitioning and simulations
Conclusions
Overview
www.mpie.de

## Slide 3
Fe-Mn based maraging TRIP steel development
TRIP: deformation-stimulated transformation of unstable austenite into martensite and accommodation plasticity (e.g. Mn, Ni, low C)
Maraging effect: hardening of heavily strained martensite via nano-sized (intermetallic) precipitates (Ni, Al, Ti, Mo)
(see also conventional Maraging steels)
* TRIP: transformation-induced plasticity
* Maraging: martensite aging
Raabe, Ponge, Dmitrieva, Sander: Adv. Eng. Mat. 11 (2009) 547
Quenched austenite: ductile low carbon martensite
Retained austenite (TRIP or TWIP)
Aging: austenite reversion (increase TRIP / TWIP volume)
Aging: controlled precipitation hardening
What is maraging-TRIP ?

## Slide 4
Low carbon: ductile martensite
Steel | C | Ni | Co | Mo | Ti | Al | Mn | Fe
Maraging | 0.01 | 18 | 12 | 4 | 1.6 | 0.15 | 0.05 | Balance
09MnPH | 0.01 | 2 | - | 1 | 1.0 | 0.15 | 9 | Balance
12MnPH | 0.01 | 2 | - | 1 | 1.0 | 0.15 | 12 | Balance
15MnPH | 0.01 | 2 | - | 1 | 1.0 | 0.15 | 15 | Balance
Precipitation Hardenable
Mn (+Ni): austenite (TRIP)
Compositions in mass%
PH
PH
PH
D. Raabe et al. Scripta Materialia 60 (2009) 1141
Martensite aging after quenching at 450°C

## Slide 5
Motivation and alloy design
Atom probe tomography
Mechanical properties and microstructure
Mn partitioning and simulations
Conclusions
Overview
www.mpie.de

## Slide 6
Atom Probe Tomography (APT)
Tip-shaped sample
initiated evaporation by
200 nm
Detector
or
+
_
~ 10 kV
3D atom map
Mass to charge ratio
Counts
APT: Time of flight measurement
(chemical identification)
+
Ion projection microscopy
(determination of position)

## Slide 7
Motivation and alloy design
Atom probe tomography
Mechanical properties and microstructure
Mn partitioning and simulations
Conclusions
Overview
www.mpie.de

## Slide 8: Hierarchy of maraging TRIP / TWIP steels
martensite
austenite
10 µm
450°C/48h
e = 0 %
Precipitation-hardening of
martensite  “maraging“
martensite
martensite
austenite
martensite
austenite
10 µm
10 µm
450°C/48h
e = 15 %
TRIP effect
hardness
+ ductility
Al
Mn
Dmitrieva et al. Acta Mater 59 (2011)

## Slide 9
Motivation and alloy design
Atom probe tomography
Mechanical properties and microstructure
Mn partitioning and simulations
Conclusions
Overview
www.mpie.de

## Slide 10
APT results: Atomic map (12MnPH aged 450°C/48h)
Mn atoms
Ni atoms
Mn iso-concentration: 18 at.%
70 million ions
Laser mode
(0.4nJ, 54K)
Dmitrieva et al. Acta Mater 59 (2011)
Martensite decorated by precipitations
Austenite
?
?

## Slide 11
M
A
Mn layer 1
Mn layer 2
Mn layer 2
Mn layer 1
Mn iso-concentration (18 at.% Mn)
Thermo-Calc 
equilibrium Mn-conc.:
27 at. % Mn in austenite (A)
3 at. % Mn in ferrite (martensite) (M)
M
A
M
depletion zone
nominal 12 at.% Mn
Aging-induced austenite reversion
Dmitrieva et al. Acta Mater 59 (2011)

## Slide 12
precipitates in a`
no precipitates in
12MnPH after aging (48h 450°C)
Raabe, Ponge, Dmitrieva, Sander: Adv. Eng. Mat. 11 (2009) 547

## Slide 13
M
A
Mn layer 1
Mn layer 2
nominal 12 at.%
phase boundary
aging
DICTRA
A
M
Thermo-Calc 
equilibrium Mn-conc.:
27 at. % Mn in austenite (A)
3 at. % Mn in ferrite (martensite) (M)
Excellent agreement between
experiment & simulation !
Aging-induced austenite reversion
Dmitrieva et al. Acta Mater 59 (2011)
Kinetic freezing and
associated austenite reversion !

## Slide 14
Mean diffusion path of Mn in austenite
(aging 450°C/48h)  2 nm
10 nm
Mn-rich
layer
A
M
PB migration
Mn diffusion
New
austenite
(formed during aging)
original position
phase boundary
final position
phase boundary
APT results and simulation: DICTRA/ThermoCalc
Dmitrieva et al. Acta Mater 59 (2011)
Notes: In order to understand the dynamics of the formation of the Mn-enriched layers on the phase boundaries, we consider the phase equilibrium contents of Mn. The averaged content of Mn measured for the Mn-enriched layers is about 26 at. %. This content corresponds to the phase equilibrium content of this element in the austenite which is 26.7 at. %. As known, local phase equilibrium can be easily reached on the grain/phase boundaries. Thus, right on the phase boundary, the equilibrium composition in austenite is reached, and a local phase transformation from martensite to austenite within the Mn-enriched layer can be expected.
However, the
With the growth of the Mn-enriched layer towards the martensitic grain, the material within the layer becomes austenitic and, thus, the phase boundary moves. The final thickness of the Mn-enriched layer is about 20 nm, thus, the phase boundary moved 20 nm during the aging treatment.
The layer-to-austenite interface provides the information about the position of the original phase boundary between the retained austenite and the martensite before aging. Further diffusion of Mn into austenite during aging was suppressed just beyond the crystallographic BCC/FCC boundary. The martensite-to-layer interface, however, indicates the position of the final phase boundary when the Mn diffusion was stopped by the water quenching after the aging treatment. The Mn enriched area in-between these two layers therefore can be addressed as additional austenite formed during the aging.
The growth of the austenite leads to an enhancement of austenite volume fraction during aging. This can be correlated to the growth of the existing austenite grains where the phase boundaries serve as nucleation seeds. We assumed an epitaxial formation of reverted austenite on the phase boundary of the retained austenite.

## Slide 15
Motivation and alloy design
Atom probe tomography
Mechanical properties and microstructure
Mn partitioning and simulations
Conclusions
Overview
www.mpie.de

## Slide 16
Conclusions
Maraging-TRIP as a new GPa steel design approach
Unexpected simultaneous increase in strength and elongation
Mn partitioning, predicted by ThermoCalc/DICTRA
Austenite stability predicted using ab initio methods (see talk of T. Hickel)
B2 and L21 nano-precipitates
Next steps: lean composition, interstitials, alloy variants, equilibrium partitioning, nano-precipitates
Mn atoms
Ni atoms
Mn iso-concentration surfaces at 18 at.%
martensite with precipitates
martensite with precipitates
70 million ions
Laser mode
(0.4nJ, 54K)
martensite with precipitates
austenite
Raabe, Ponge, Dmitrieva, Sander: Adv. Eng. Mat. 11 (2009) 547