## Slide 1
D. Ponge, J. Millan, L. Yuan, S. Sandlöbes, A. Kostka, P. Choi, T. Hickel, J. Neugebauer, D. Raabe
Düsseldorf, Germany
WWW.MPIE.DE
d.raabe@mpie.de
30. Nov. 2011 Dierk Raabe GDCh Kolloquium Universität Duisburg-Essen
Nanostructuring of 100 thousand tons

## Slide 2
Nanostructures in 100 thousand tons
www.mpie.de
Agitation: metallic alloys in 10 minutes
Self-organized nanostructuring: partitioning, kinetic freezing, adsorption isotherm

## Slide 3: The Düsseldorf Local Electrode Atom Probe (LEAP) Laboratory
LEAP 3000X HR, IMAGO Sci. Instr.
(since February 2009)
High spatial resolution
(Dx ~ 0.2 nm, Dz ~ 0.1 nm)
High mass resolution
(Dm/m = 1100, FWHM at 27 Da)
Fast data acquisition rate
(max. ~ 2 Mio ions / min)
Large probed volumes
(max. ~ 200 x 200 x 1000 nm3)
High detection sensitivity
(min. ~ 10 ppm)
Pulsed laser
(l = 532 nm, ~ 10 ps)
2/55

## Slide 4
Titanium
Aluminium
Magnesium
Nickel
Steels
Intermetallics
New materials for key technologies: Aero-space

## Slide 5
New materials for key technologies: mobility on land and water
Steels
Magnesium
Aluminium
Titanium

## Slide 6
New materials for key technologies: Power plants
Steels
Nickel
Intermetallics

## Slide 7
New materials for key technologies: Health
Titanium
Magnesium
Copper
steels

## Slide 8
From atomistic understanding towards designing new materials
D. Raabe et al. Scripta Materialia 60 (2009) 1141

## Slide 9
as-quenched
aged 450°C/48h
-Fe (Martensite)
-Fe (Austenite), vol. fraction 15-20%
increase of austenite
fraction during aging
Precipitation
hardening
strain 0%
1
1
strain 15%
2
2
?
Effect of aging on ductility
D. Raabe et al. Scripta Materialia 60 (2009) 1141
Notes: Stress- strain curves for the Maraging TRIP alloy. It has up to 15 vol. % retained austenite prior to deformation which is gradually reduced during straining and provide for a high dictility. After the aging heat treatment, the alloy shows an unexpected effect that the ultimate tensile strength and the total elongation simultaneously increase. The increase in the strength is mainly attributed to the formation of the nano-precipitates and to the following precipitation hardening of the martensite. However, as one of the possible reasons for the partial increase in ductility we consider a delayed austenitization, means that the volume fraction of austenite grows during the aging.
Other reasons: tempering of the as-quenched martensitic microstructure: reduced micro-strains; high strain hardening rate: local hardening due to Orowan loops formation, preventing the necking.

## Slide 10
12MnPH X-Ray
Effect of cold rolling after aging
g formation
during aging
450°C/48h
g->a’ (TRIP)
D. Raabe et al. Scripta Materialia 60 (2009) 1141
Why so much austenite 120 K below equilibrium transformation?
Notes: X-ray: 12Mn PH:
90% a‘-martensite
4% e-martensite
7% retained austenite

## Slide 11
M
A
Mn layer 1
Mn layer 2
Mn layer 2
Mn layer 1
Mn iso-concentration (18 at.% Mn)
Thermo-Calc 
equilibrium Mn-conc.:
27 at. % Mn in austenite (A)
3 at. % Mn in ferrite (martensite) (M)
M
A
M
depletion zone
nominal 12 at.% Mn
Aging-induced austenite reversion
Dmitrieva et al. Acta Mater 59 (2011)

## Slide 12
M
A
Mn layer 1
Mn layer 2
nominal 12 at.%
phase boundary
aging
DICTRA
A
M
Thermo-Calc 
equilibrium Mn-conc.:
27 at. % Mn in austenite (A)
3 at. % Mn in ferrite (martensite) (M)
Excellent agreement between
experiment & simulation !
Aging-induced austenite reversion
Dmitrieva et al. Acta Mater 59 (2011)
Kinetic freezing and
associated austenite reversion !
Can I push this idea further ?

## Slide 13: Martensite relaxation & aging & nanoscale austenite reversion
Ultra high strength and corrosion resistance
650 MPa to 2 GPa
400°C aging: Ms-relaxation + prec. (aging) + austenite reversion
Fe-13.6Cr-0.44C (wt.%)

## Slide 14: Martensite relaxation & aging & nanoscale austenite reversion
at 5.45 at.% C, austenite forms at 400°C
C has ‘/\’ shape in austenite layer: inheritance from austenite, Gibbs adsorption isotherm;
C on martensite grain boundaries
C has ‘V’ shape in austenite layer: austenite reversion through partitioning and kinetic freezing

## Slide 15
Self-repair steels

## Slide 16
Answering societies' grand challenges with complex alloys
www.mpie.de
70% of all industrial innovations are associated with progress in
materials science and engineering
Specifically, metallic materials occupy key roles
(energy, transportation, health, safety, infrastructure)
Our mission: Designing new metallic alloys from first principles
Multiscale simulation
Multiscale characterization starting from the atomic scale
Synthesis, processing, testing