## Slide 1
D. Raabe, F. Roters, P. Eisenlohr, H. Fabritius, S. Nikolov, M. Petrov
O. Dmitrieva, T. Hickel, M. Friak, D. Ma, J. Neugebauer
Düsseldorf, Germany
WWW.MPIE.DE
d.raabe@mpie.de
IHPC - Institute for High Performance Computing Singapore 1. Nov 2010 Dierk Raabe
Using ab-initio based multiscale models and experiments for alloy design

## Slide 2
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges
Overview
Raabe: Adv. Mater. 14 (2002), Roters et al. Acta Mater.58 (2010)

## Slide 3
Ab initio and crystal modeling
Counts, Friák, Raabe, Neugebauer: Acta Mater. 57 (2009) 69
Electronic rules for alloy design: Add electrons rather than atoms
Obtain data not accessible otherwise
Combine to atomic scale experiments
Most exact known materials theory
Can be used at continuum scale

## Slide 4
Time-independent Schrödinger equation
h/(2p)
Many particles (stationary formulation)
Square ¦y(r)¦2 of wave function y(r) of a particle at given position r = (x,y,z) is a measure of probability to observe it there
Raabe: Adv. Mater. 14 (2002)

## Slide 5
i electrons: mass me ; charge qe = -e ; coordinates rei
j atomic cores: mass mn ; charge qn = ze ; coordinates rnj
Time-independent Schrödinger equation for many particles
Raabe: Adv. Mater. 14 (2002)

## Slide 6
Adiabatic Born-Oppenheimer approximation
Decoupling of core and electron dynamics
Electrons
Atomic cores
Raabe: Adv. Mater. 14 (2002)

## Slide 7
Hohenberg-Kohn-Sham theorem:
Ground state energy of a many body system definite function of its particle density
Functional E(n(r)) has minimum with respect to variation in particle position at equilibrium density n0(r)
Chemistry Nobelprice 1998
Hohenberg Kohn, Phys. Rev. 136 (1964) B864

## Slide 8
Total energy functional
T(n) kinetic energy
EH(n) Hartree energy (electron-electron repulsion)
Exc(n) Exchange and correlation energy
U(r) external potential
Exact form of T(n) and Exc(n) unknown
Hohenberg Kohn, Phys. Rev. 136 (1964) B864

## Slide 9
Local density approximation – Kohn-Sham theory
Parametrization of particle density by a set of ‘One-electron-orbitals‘
These form a non-interacting reference system (basis functions)
Calculate T(n) without consideration of interactions
Determine optimal basis set by variational principle
Hohenberg Kohn, Phys. Rev. 136 (1964) B864

## Slide 10
Ab initio: theoretical methods
Density functional theory (DFT), generalized gradient approximation (GGA); also LDA
Vienna ab-initio simulation package (VASP) code or SPHINX; different pseudo-potentials, Brillouin zone sampling, supercell sizes, and cut-off energies, different exchange-correlation functions, M.-fit
Entropy: non-0K, dynamical matrix, configuational analytical
Hohenberg Kohn, Phys. Rev. 136 (1964) B864

## Slide 11
Ab initio: typical quantities of interest in materials mechanics
Lattice structures (e.g. Polymers, carbides, Laves)
Lattice parameter (e.g. alloys, solute limits)
Ground state energies of phases, free energies
Elastic properties
Simple defect structures and formation energies, e.g. vacancies, interstitials, dislocation cores
Energy landscapes for athermal transformations
Raabe: Adv. Mater. 14 (2002)

## Slide 12
Raabe, Zhao, Park, Roters: Acta Mater. 50 (2002) 421
Theory and Simulation: Multiscale crystal mechanics

## Slide 13
Overview
Raabe: Adv. Mater. 14 (2002), Roters et al. Acta Mater.58 (2010)
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges

## Slide 14
115 GPa
20-25 GPa
Stress shielding
Elastic Mismatch:
Bone degeneration, abrasion, infection
Raabe, Sander, Friák, Ma, Neugebauer: Acta Mater. 55 (2007) 4475
BCC Ti biomaterials design

## Slide 15
Design-task: reduce elastic stiffness
Raabe, Sander, Friák, Ma, Neugebauer: Acta Mater. 55 (2007) 4475
M. Niinomi, Mater. Sci. Eng. 1998
Bio-compatible elements
BCC Ti biomaterials design
From hex to BCC structure: Ti-Nb, …

## Slide 16: Construct binary alloys in the hexagonal phase
Raabe, Sander, Friák, Ma, Neugebauer: Acta Mater. 55 (2007) 4475

## Slide 17: Construct binary alloys in the cubic phase
Raabe, Sander, Friák, Ma, Neugebauer: Acta Mater. 55 (2007) 4475

## Slide 18
MECHANICAL
INSTABILITY!!
Ultra-sonic measurement
exp. polycrystals
bcc+hcp phases
Ti-hex: 117 GPa
theory: bcc
polycrystals
XRD
DFT
polycrystal Young`s modulus (GPa)
Raabe, Sander, Friák, Ma, Neugebauer, Acta Materialia 55 (2007) 4475
Elastic properties / Hershey homogenization
hex
bcc

## Slide 19
Ti-18.75at.%Nb
Ti-25at.%Nb
Ti-31.25at.%Nb
Az=3.210
Az=2.418
Az=1.058
[001]
[100]
[010]
Young‘s modulus surface plots
Pure Nb
Az=0.5027
Az= 2 C44/(C11 − C12)
Ma, Friák, Neugebauer, Raabe, Roters: phys. stat. sol. B 245 (2008) 2642
Hershey
FEM
FFT
Ab initio alloy design: Elastic properties: Ti-Nb system

## Slide 20
More than one million hip implants per year:
Take-home message
elastically compliant Titanium-alloys can reduce surgery
www.mpie.de

## Slide 21
Overview
Raabe: Adv. Mater. 14 (2002), Roters et al. Acta Mater.58 (2010)
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges

## Slide 22
Stress s [MPa]
1000
800
600
400
200
0
0 20 40 60 80 100
Strain e [%]
TRIP
steel
TWIP steel
Ab-initio methods for the design of high strength steels
www.mpie.de
martensite
formation
twin formation
Hickel, Dick, Neugebauer

## Slide 23
www.mpie.de
Ab-initio methods for the design of high strength steels
C
A
B
B
C
Hickel, Dick, Neugebauer

## Slide 24
Develop new materials via ab-initio methods
www.mpie.de
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges

## Slide 25
Nano-precipitates in soft magnetic steels
size Cu precipitates (nm)
{JP 2004 339603}
15 nm
magnetic loss (W/kg)
Fe-Si steel with Cu nano-precipitates
nanoparticles too small for Bloch-wall interaction but
effective as dislocation obstacles
mechanically very strong soft magnets for motors

## Slide 26
Cu 2 wt.%
20 nm
120 min
20 nm
6000 min
Iso-concentration surfaces for
Cu 11 at.%
Fe-Si-Cu, LEAP 3000X HR analysis
Fe-Si steel with Cu nano-precipitates
450°C aging

## Slide 27
Modeling: ab-initio, DFT / GGA, binding energies
Fe-Si steel with Cu nano-precipitates
Notes: 26

## Slide 28
Modeling: ab-initio, DFT / GGA, binding energies
Fe-Si steel with Cu nano-precipitates
Notes: 27

## Slide 29
Modeling: ab-initio, DFT / GGA, binding energies
Fe-Si steel with Cu nano-precipitates
Notes: 28

## Slide 30
Modeling: ab-initio, DFT / GGA, binding energies
Fe-Si steel with Cu nano-precipitates
Notes: 29

## Slide 31
Ab-initio, binding energies: Cu-Cu in Fe matrix
Fe-Si steel with Cu nano-precipitates

## Slide 32
Ab-initio, binding energies: Si-Si in Fe matrix
Fe-Si steel with Cu nano-precipitates

## Slide 33
For neighbor interaction energy take difference (in eV)‏
(repulsive) = 0.390
(attractive) = -0.124
(attractive) = -0.245
Ab-initio, binding energies
Fe-Si steel with Cu nano-precipitates

## Slide 34
Ab-initio, use binding energies in kinetic Monte Carlo model

## Slide 35
Develop new materials via ab-initio methods
www.mpie.de
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges

## Slide 36
Counts et al.: phys. stat. sol. B 245 (2008) 2630
Counts, Friák, Raabe, Neugebauer: Acta Mater. 57 (2009) 69
Ab-initio design of Mg-Li alloys
Y: Young‘s modulus
r: mass density
B: compressive modulus
G: shear modulus
Weak under normal load
Weak under
shear load

## Slide 37
Develop new materials via ab-initio methods
www.mpie.de
Ab initio in materials science: what for ?
Ab initio to continuum models (mechanics)
Titanium (ab initio and continuum)
Mn-steels (identify mechanisms)
Steel with Cu precipitates (atom scale experiments)
Mg-Li alloy design (ab initio property maps)
Singapore crab (ab initio and homogenization)
Conclusions and challenges

## Slide 38
Length [m]
10-9
10-6
10-3
100
10-15
10-9
10-3
103
Time [s]
Boundary conditions
Crystals and anisotropy
Kinetics of defects
Structure of defects
Structure
of matter
D. Raabe: Advanced Materials 14 (2002) p. 639
Scales in computational crystal plasticity

## Slide 39
* DFT: density functional theory
Raabe, Sander, Friák, Ma, Neugebauer: Acta Mater. 55 (2007) 4475
From ab-initio to polycrystal mechanics
Gb, Gb2 , ...
<E>